Experiment 3:  Tensile Test on Cold-Rolled Steel

OBJECTIVE:  The main objective of the experiment was to observe the effects of stress and strain of the cold-rolled steel rod when axially loaded to failure.

DATA:  Tables 1 through 3 show the raw data collected during the experiment.

Table 1: Rod Diameters		                                                                   Figure 1:  Strain Gage Indicator

| Diameter | Length (in) |
| --- | --- |
| Initial 1 | 0.622 |
| Initial 2 | 0.621 |
| Final | 0.488 |

Table 2:  Strain Values

| Load (kips) | Axial Strain (micro-strain) | Load (kips) | Axial Strain (micro-strain) |
| --- | --- | --- | --- |
| 2 | 288 | 20 | 2247 |
| 4 | 498 | 21 | 2349 |
| 6 | 709 | 22 | 2512 |
| 8 | 927 | 23 | 2793 |
| 10 | 1146 | 24 | 3297 |
| 12 | 1359 | 25 | 3992 |
| 14 | 1569 | 26 | 5192 |
| 15 | 1680 | 26.5 | 6346 |
| 16 | 1754 | 27 | 8378 |
| 17 | 1861 | 27.3 | 11900 |
| 18 | 1979 | 27.8 | 18000 |
| 19 | 2093 |  |  |

Table 3:  Load Characteristics

| Stress Type | Load (lbs) |
| --- | --- |
| Ultimate | 28300 |
| Failure | 2100 |

T

RESULTS:  Tables 4 and 5 and Figure 2 represent the calculated results from the raw data.

Table 4:  Calculated Stresses		Figure 2:  Stress vs Strain

| Load (kips) | Stress (ksi) | Load (kips) | Stress (ksi) |
| --- | --- | --- | --- |
| 2 | 6.593 | 20 | 65.926 |
| 4 | 13.185 | 21 | 69.222 |
| 6 | 19.778 | 22 | 72.519 |
| 8 | 26.370 | 23 | 75.815 |
| 10 | 32.963 | 24 | 79.111 |
| 12 | 39.556 | 25 | 82.408 |
| 14 | 46.148 | 26 | 85.704 |
| 15 | 49.445 | 26.5 | 87.352 |
| 16 | 52.741 | 27 | 89.000 |
| 17 | 56.037 | 27.3 | 89.989 |
| 18 | 59.334 | 27.8 | 91.637 |
| 19 | 62.630 |  |  |

Table 5:  Stress Types

| Stress Type | Stress (ksi) |
| --- | --- |
| Ultimate | 93.28 |
| Engineering Failure | 69.22 |
| True Failure | 112.28 |

CONCLUSION:

The material tested is a ductile material because of its yielding capabilities.  Any error that occurred in the lab was most likely human error.  This occurred either from improper reading of the strain gage indicator or improper placement of the strain gage indicator.